## Slide 1
Status of TI Materials

## Slide 2: Topology & Topological Invariant
Not continuously deformable
Topological
Invariant
Number of Holes
Manifold of wave functions in the Hilbert space
rxy
rxx
Quantum Hall system:
D. Hilbert
K. von Klitzing
“Nontrivial”
topology
Bulk acquires a
Landau-Level gap
H

## Slide 3
Topological Insulators
Chern number: n
Re un
0
Im un
un(k)
kx
-p
ky
0
p
Brillouin zone
Complex
plane
ky
p
0
L1
L2
L3
L4
p
kx
Z2 invariant: n (= 0 or 1)
w.f. parity at Li :
x (Li)
Magnetic Field
k
Energy
k = 0
Bulk Conduction Band
Bulk Valence Band
up spin
down
spin
Dirac point
+
+
-
+
Quantum Hall System
2D Topological Insulator
n = 2
n = 1

## Slide 4
Topological Insulators
Chern number: n
Re un
0
Im un
un(k)
kx
-p
ky
0
p
Brillouin zone
Complex
plane
ky
p
0
L1
L2
L3
L4
p
kx
Z2 invariant: n (= 0 or 1)
w.f. parity at Li :
x (Li)
Magnetic Field
+
+
-
+
Quantum Hall System
3D Topological Insulator
n = 2
E
2D Dirac cone
Helical spin
polarization

## Slide 5: 3D Topological-Insulator Materials
Bi1-xSbx
Fu & Kane, PRB (2007)
Band Inversion
x = 0.10
Hsieh et al., Nature (2008)
Bonding
CF
SOC
Bi2Se3
Zhang et al.,
Nat. Phys.
(2009)
Xia et al.,
Nat. Phys.
(2009)
BCB
BVB

## Slide 6: Bi2Se3
Stanford-NHMFL Collaboration
Sb-doped Bi2Se3
Surface contribution ~0.1%
Analytis et al., Nature Physics (2010)
BCB
BVB
EF

## Slide 7
Chalcogen ordering leads to characteristic peaks .
Important Theme in TI Research：
How to reduce bulk carriers and
achieve a bulk-insulating state
Bi2Te2Se
q-dependence signifies that the Fermi surface is 2D.
Activation behavior above 150 K with
D = 23 meV
Nominally stoichiometric
crystals of Bi2Se3 : n-type
Bi2Te3 : p-type
Surface contribution is ~6% !
Ren, Ando et al., PRB (2010)

## Slide 8
Bi2-xSbxTe3-ySey
Ren, Ando et al., PRB (2011)
Bi1.5Sb0.5Te1.7Se1.3
Thickness Dependence
Taskin, Ando et al., PRL (2011)
Surface-Dominated Transport
In the 8-m-thick sample,
the surface contribution is 70%!

## Slide 9: ARPES on Bi2-xSbxTe3-ySey
y
Arakane, Sato, Ando et al.,
Nature Commun. (2012)

## Slide 10: Spin Pumping
Symmetrical signal is due to bulk Seebeck effect caused by heating.
Spin-Electricity Conversion from
Spin-Momentum Locking
Shiomi, Saitoh, Ando et al., PRL (2014)

## Slide 11: BSTS Spin-MR Device (Kyoto)
Bi2Se3
+I
-I
Ando, Shiraishi, Ando et al., Nano Lett. (2014)

## Slide 12
Bi2Se3 Thin Films

## Slide 13
40-nm thick film
Taskin, Ando et al., Adv. Mater. (2012)
Bi2Se3

## Slide 14: MBE-Grown Bi2Se3 Fimls
50-nm thick film
2D
Dirac
10-nm thick Film
graphene
graphite

## Slide 15: Surface Morphology Across tc
3-nm Film
5-nm Film
8-nm Film
Taskin, Ando et al., PRL (2012)

## Slide 16: Topological Protection
Hybridization of top and bottom surfaces
Bottom surface
Top surface
Top surface
Bottom surface
hybridize
Surface states become degenerate.
EF
 No protection from backscattering.
Y. Zhang, Q.K. Xue et al., Nat. Phys. (2010)
k
Energy
k = 0
Bulk Conduction Band
Bulk Valence Band
up spin
down
spin
Dirac point
EF
Protection from
backscattering

## Slide 17: Topological Protection
Hybridization of top and bottom surfaces
Bottom surface
Top surface
Top surface
Bottom surface
hybridize
Surface states become degenerate.
EF
Manifestation of the “topological protection”
Taskin, Ando et al., PRL (2012)
 No protection from backscattering.
k
Energy
k = 0
Bulk Conduction Band
Bulk Valence Band
up spin
down
spin
Dirac point
EF
Protection from
backscattering

## Slide 18
(Bi1-xSbx)2Te3 Thin Films
Zhang et al., Nat. Commun. (2011)

## Slide 19: Top-Gate Device
Bi2-xSbxTe3 Thin Film (30-nm thick)
in situ capped with ~5-nm Al2O3
(Dielectric layer: 200-nm SiNx)
Yang, Ando et al., APL (2014)

## Slide 20: Bottom-Gate Device
Bi2-xSbxTe3 Thin Film (~20-nm thick)
m
Top
Bottom
m
Top
Bottom
150-nm SiO2
Dielectric layer
Top Gate

## Slide 21: Dual-Gate Device
Bi2-xSbxTe3 Thin Film (~20-nm thick)
Bottom
Gate
Top Gate
Dual Gate
m
Top
Bottom
Yang, Ando et al.,
ACS Nano (2015)

## Slide 22
Topological Crystalline Insulator
… New Type of TI

## Slide 23: Topological Crystalline Insulator SnTe
SnTe
Hsieh et al., Nature Commun. (2012)
PbTe
SnTe
: contribution from Te p-orbital
SnTe
PbTe
Band inversion + Mirror symmetry
 Nontrivial Mirror Chern number
ky
p
0
L1
L2
L3
L4
p
kx
+
-
-
+
Z2 invariant n = 0
Tanaka, Sato, Ando et al.,
Nature Physics (2012)

## Slide 24: SnTe (111) Surface State
Tanaka, Sato, Ando et al., PRB (2013)

## Slide 25: SnTe (111) Surface State
Tanaka, Sato, Ando et al., PRB (2013)
Two Different Dirac Cones at G and M

## Slide 26: SdH Oscillations in SnTe (111) Films
2D
SnTe surface
n++-Bi2Te3 30 nm
p++-SnTe 36 nm
Sapphire
0.55
Taskin, Ando et al.,
PRB (2014)
Dirac
n-type carriers

## Slide 27: SdH Oscillations in SnTe (111) Films
0.55
n-type carriers
2D
Dirac
kF = 1.8 106 cm-1
& 2.1 106 cm-1
Dirac fermions on the top SnTe surface
Taskin, Ando et al.,
PRB (2014)

## Slide 28
Topological Superconductor

## Slide 29: Possible Topological Superconductors
Z
Time-Reversal Invariant (TRI)
Time-Reversal Broken (TRB)
1D
2D
3D
Z2
Z2
Z2
Z
-
Schnyder-Ryu-Furusaki-Ludwig (2008)
Kitaev (2009)
“Periodic Table” of topological invariant
Chiral p-wave
SC in TI surface
Surface State of TIs
Bogoliubov qp
EF
TI
SC
SC
f = 0
f = p
Fu & Kane (2008)
EF
2D
Majorana
Edge State
Sr2RuO4
(D)
(DIII)

## Slide 30
2012
Bi2Te3
n-type, 81019 cm-3
Nb
Clean limit  evidence for surface?

## Slide 31
IcRN is ~10 times smaller than expected
IcRN scales inversely with W
Bc (1st minimum) is ~5 times smaller than expected
Bi2Se3
, n-type, 81017 cm-3

## Slide 32
14-nm-thick (Bi,Sb)2Se3
TCNQ surface doping
Back-gating
Ti(2.5 nm)/Al(140 nm)
Finite supercurrent through surface state
F/F0 ~ 0.23 n
Flux focusing?
2013

## Slide 33
T-dep. of Ic gives evidence for ballistic junction through the surface state
Small IcRN is explicable if the surface channel dictates RN

## Slide 34
Bi2Se3, n-type
9-nm thick
n2D=1013-1014 cm-2
Back gating
L = 230 nm
Andreev reflection
Fabry-Perot oscillations
ZBCP similar to that in 1D SOC nanowire
(weak antilocalization?)
Phase-coherent transport in TI
 Due to topological protection of the surface state?

## Slide 35
Bulk-insulating BSTS flake, 80 – 200 nm thick
Junction width and length: ~50 nm
IcRN is only 7 mV 
Mean free path: 10 – 40 nm
Low transparency
Diffusive transport through surface

## Slide 36
Zero-bias anomaly  induced SC?
No supercurrent in this experiment
50 or 70 nm-thick HgTe  3D TI
DNb = 1 meV, Andreev reflection
Precursor to Fraunhofer pattern?
Sample with improved interface

## Slide 37
fluctuations originate from Josephson effect
Supercurrent through the surface state
Only 2p periodicity
No signature of Majoranas, which is reasonable for a large number of unprotected modes
70 nm-thick
HgTe as 3D TI

## Slide 38
Skewness (due to the 2nd harmonic) remains the same for varying W and L
Fits very well to ballistic junction model
 Josephson current is carried by ABS with high transmittance, which is possibly related to the helical nature of the surface state
No inverse proximity effect
 Absence of bulk states

## Slide 39
2D TI

## Slide 40
Evidence for supercurrents through the 1D helical edge state
m in the bulk CB
2D TI, 7.5-nm HgTe
W = 4 mm
L = 800 nm
m in the bulk gap
Similar result for InAs/GaSb
arXiv:1408.1701

## Slide 41
Ferromagnetic Atomic Chain

## Slide 42
Fe chain on Pb(110)
Odd number of crossings
Spin-polarized STM
SC Tip (high resolution)
 p-wave gap ~ 0.3 meV
FM chain
+ Rashba SOC in s-wave SC